## Slide 1: The effect of the non-adiabatic phonon on Tc in -NbN inside and outside a cavity
Qinyan Yi
Peking University, China
(an intern project in Prof. Angel Rubio’s research group from Sep. to Nov. 2023)
Supervised by Dr. I-Te Lu, Dr. Hannes Huebener, and Prof. Angel Rubio

## Slide 2: Introduction (motivation and goal)
NbN is a good superconducting material with a relatively high transition temperature. Its notable superconductivity and mechanical properties make it have various technological applications.
Non-adiabatic (dynamical) phonon takes into account the propagation time for the force acting on nucleus due to the atom displacement. This leads to a change in phonon frequencies, thus change Tc.
Light-matter interaction change (adiabatic and non-adiabatic) phonon dispersions, leading to the change in Tc of NbN inside a cavity.

## Slide 3: Crystal structure and electronic band structure of -NbN
Nb
N
unit cell of -NbN
Band structure of -NbN

## Slide 4: Phonon-dispersion of -NbN
Phonon instability issue can be avoided by using 1) a pseudopotential of Nb with 40.5 nuclear charge or 2) electrons taken out from the unit cell
phonon-dispersions calculated by ph.x using different smearing and pseudopotentials

## Slide 5: Phonon-dispersion of -NbN
phonon-dispersion of -NbN inside and outside a cavity
Adiabatic phonon calculated by ph.x, non-adiabatic phonon calculated by EPIq. Non-zero frequencies at gamma point are probably caused by numerical error. Following Eliashberg function calculations show that this does not affect Tc much.

## Slide 6: Anisotropic superconducting gaps
Anisotropic superconducting gaps from the anisotropic Midgal-Eliashberg equations shows that the superconducting gaps are isotropic => use the isotropic Eliashberg equations to reduce computational cost
Eliashberg equations
k-resolved superconducting gap of 𝛿-NbN calculated by anisotrpic Eliashberg equations

## Slide 7: Isotropic Eliashberg spectral function, electron-phonon couplings, and superconducting temperature
light-matter coupling:
3 phonon modes: (1,0,0), (0,1,0), (0,0,1)
Tc calculated by McMillan-Allen-Dynes
formula

## Slide 8: Summary of this project
The imaginary phonon frequencies in low temperature indicate that pure -NbN would become unstable. The instability is avoided by 1) using a larger smearing or 2) applying virtual crystal approximation through a pseudopotential of 40.5 nuclear charge for Nb or taking out 0.5 electron from the unit cell.
Considering the non-adiabatic effect can lower the critical temperature from 23.5K to 21.2K, but it’s still higher than the experiment result 17.3K.
Putting -NbN inside a cavity can change its critical temperature by light-matter interaction. For the case in our calculation, Tc becomes about 0.5K lower.